## Slide 1: Optimization of print parameters to reduce warpage in fused deposition modeling
Pranav Addepalli

## Slide 2: Background
3D printing is crucial for many industries
  Construction
  Medicine
  Robotics
  Aerospace
  Defense
http://www.3dprinterworld.com/article/3d-printing-enables-university-students-become-aerospace-manufacturers

## Slide 3: Background
Fused Deposition Modeling
  Most common printing method
  Melts a thermoplastic filament repeatedly
Polylactic Acid
  Most common filament
  Made from renewable lactic acid
https://www.3dnatives.com/en/fused-deposition-modeling100420174/

## Slide 4: Background
FDM prints layer by layer, creating thermal cycles
  Cooling  Contraction  Mechanical stress
  Heating  Expansion  Mechanical stress
  Greatest stress in corners
This is called warpage
https://www.3dhubs.com/talk/t/adhesion-and-upward-warping-problems/4334

## Slide 5
Thermal properties are important to understand!

## Slide 6: My Project
Studying multiple print parameters
  Wall thickness
  Layer height
  Infill percentage
  Infill height
Effect on temperature distribution
PLA discs during printing process
https://www.dddrop.com/wp-content/uploads/2018/02/3D-printen-stevige-infill.jpg

## Slide 7: My Project
Optimizing values for the print parameters
Deep Learning
  Visualize, model, find trends
  in spatiotemporal temperature data and heat flow trajectories
Find the best parameters and print test discs

## Slide 8: Variables
Infill type (grid vs. triangular)
Infill percentage (10%, 20%, 30%)
https://3dprinting.com/tips-tricks/how-to-choose-an-infill-for-your-3d-prints/
http://tcadsolutions.com/3dprinting.html

## Slide 9: Variables
Wall thickness (0.4mm vs. 0.8mm)
Layer height (0.1mm vs. 0.2mm)
http://archive.fabacademy.org/fabacademy2017/fablabvigyanashram/students/132/assignments/assignment%205.html
https://medium.com/3d-printing-in-o-p/iv-slicing-72a9515f44bc

## Slide 10: Materials
NTC Thermistors
Hatchbox PLA
Arduino Uno R3 (with breadboard)
NVIDIA Jetson Nano
gCreate gMax 1.5 XT+

## Slide 11: 5 Phase Procedure
Design
Data Collection
Modeling
Optimization
Final Tests

## Slide 12: 1) Design
Design CAD models in Fusion 360
  8 inch diameter
  0.5 inch thickness
  Channels along circles for thermistors
Slice disc with different print parameters in Ultimaker Cura

## Slide 13: 2) Data Collection
Halfway through the printing process:
  Embed thermistors
  Connect to Arduino
  Begin recording temperature

## Slide 14: 3) Modelling
Similar to the data from junior year
More parameters and tests  can find trends in the data
  Deep learning (ANNs, DTW, Getis-Ord GI*, etc.)
  Heat flow trajectory analysis

## Slide 16: 4) Optimization
Method will be refined later
Optimization, simply: reducing the value of a cost function by changing some inputs
Inputs: print parameters
Cost function f : Euclidian distance from geometric center to a weighted temperature center at time t
(a basic framework for it)
https://justinbradley.unl.edu/cps-co-optimization

## Slide 17: 4) Optimization
The full process I use depends on what the data looks like, but…
Assuming f is:
  non-convex (not always above its tangent),
  non-smooth (gradient can be undefined at some points),
  noisy (in blue),
  well-conditioned (scale of input values is known)
  and numerically unknown,
(a more complex framework for it)
  We have a very difficult problem.
https://scipy-lectures.org/advanced/mathematical_optimization/index.html

## Slide 18: 4) Optimization
But we can still approach this!
The Newton Method:
  uses local quadratic approximations to find which direction to “jump” to find the minimum
  uses the gradient and the Hessian
The Broyden-Fletcher-Goldfarb-Shanno algorithm (BFGS) approximates the Hessian iteratively
(a complicated framework for it)
  This gives us a quasi-Newton method for our optimization.
https://ardianumam.wordpress.com/2017/09/27/newtons-method-optimization-derivation-and-how-it-works/

## Slide 19: 5) Final Tests
Will print discs with the optimized parameters
Will study the cost function and look for a statistically significant decrease

## Slide 20
Current Progress

## Slide 21: Junior Year Conclusions and Results
Increasing infill percentage increases the uniformity of the temperature distribution and theoretically reduces warpage
Designed a process to collect spatiotemporal temperature data during 3D printing
Designed a weighted temperature centers method to analyze data

## Slide 22: Senior Year Progress
Completed Phase 1 (Design)
Working on Phase 2 (Data Collection)
Completed multiple subtasks for future phases
  built Arduino-thermistor circuit
  explored junior year data
  developed program for modelling data in Python
  started setting up Jetson
  fixed gCreate printer’s z-axis problem

## Slide 23: Future Work
Complete Phase 2 (data collection) and Phase 3 (modelling) by March 1st
  Enough for the engineering side of the project
  Can draw conclusions
Complete Phase 4 (optimization) and Phase 5 (final tests) by Symposium in May
  Computational modeling side of the project
  Will support/oppose my conclusions

## Slide 24: References
Zhang, J., Wang, X. Z., Yu, W. W., Deng, Y. H. (2017). Numerical investigation of the influence of process conditions on the temperature variation in fused deposition modeling. Materials & Design, 130, 59-68. doi:10.1016/j.matdes.2017.05.040
Deng, C., Kang, J., Shangguan, H., Hu, Y., Huang, T., Liu, Z. (2018). Effects of hollow structures in sand mold manufactured using 3D printing technology. Journal of Materials Processing Technology, 255, 516-523. doi:10.1016/j.jmatprotec.2017.12.031
Vaughan, N. & Gabrys, B. (2016). Comparing and combining time series trajectories using Dynamic Time Warping. Procedia Computer Science, 96, 465 – 474. doi:10.1016/j.procs.2016.08.106
Studer, M & Ehrig, F. (2014). Minimizing part warpage in injection molding by optimizing wall thickness distribution. Advances in Polymer Technology, 33. doi:10.1002/adv.21454